## Slide 1: Nucleation Limited Switching varying pulse width
07/23/2024

## Slide 2: Waveforms
1) PUNDp3.5
2) set
3) PUNDp3.5
Change
50 ns, 100 ns, 1 us, 10 us, 100 us, 1 ms, 10 ms, 100 ms, 1 s, and 10 s
Then change to NDPUn3.5 with positive a set pulse.
Use to construct PE loop

## Slide 3
Sample: SX19C bot
V set
PUNDp3.5
NDPUn3.5
V set
Darker color = smaller

## Slide 4
Pp: PUNDp3.5
Nn: NDPUn3.5
1 V: set pulse at 1 V
Net zero line
In general, blue is above red because .
More polarization reversal with positive , so NDPUn3.5 measures a larger switching current.

## Slide 5
Faster set pulses generate more imprint
It looks like the domains with smaller don’t switch until the pulse duration is longer?!
This means that domains with larger are unable to switch by the fast set pulses?
V
Darker color = faster set pulse
V
The reverse case is also apparent.
We expect a direct correlation between pulse duration and .